## Slide 1: Roughness in SLS Eos P500 FDR
Chances in:
build plate position
Build setup
Presence of thin walls

## Slide 2: Description of the project
EOS P500 Fine Detail Resolution (FDR)
It works with Ftheta lenses and two 50-watt CO lasers with scan speed of 10 m/sec.
Minimum layer thicknesses of 40/60 µm and minimum wall thicknesses of 0,22 mm
Lasers have beam diameter of 10.6 µm and a spot size of 5 µm
Material used is PA1101 white (glass temperature of 46 ºC and a melting temperature of 180 ºC)
Chamber at 176 ºC, build plate at 175 ºC
Techniques:
Downskin and upskin receive higher energy to keep the part together and make the surface smoother. This cannot be done for contours, where some particles can remain stuck at the border of the melting zone during the offset hatching of the laser and worsen the surface quality. For this reason, the contour is smeared with a second lower laser intensity to flatten all the unwanted stuck particles along the contour.

## Slide 3: Build plate setting
1UH
3UH
5UH
7UH
2H
4H
5H
7H
9H
1UF
3UF
5UF
1H
1F
3H
2F
3F
5F
7F
9F
2UF
2UH
4UH
6UH
8UH
9UH
11UH
13UH
11UF
11F
11H
12UF
12UH
12F
12H
13F
13UF
14UH
14F
13H
4UF
4F
6UF
6F
6H
7UF
8UF
8H
8F
9UF
10F
10H
10UF
10UH
15UH
15F
15H
15UF
16UH
16F
16UF
16H
14UF
14H
17UH
17H
17UF
17F
18UH
18F
18UF
18H
19UH
19UF
19H
19F
20UH
20F
20UF
20H
21UH
21F
21UF
21H
22UH
22F
22H
22UF
23UH
23F
23UF
23H
24UH
24F
For each circled sample we carried out:
Image sampling with Olympus LEXT OLS4100
Profile analysis with MountainSpectral® Expert and SPIP 6.7.9
Taguchi Array Design L16(8^1 2^2) with 3 factors and 16 runs

## Slide 4: Roughness measurements
Roughness has been investigated through Ra, Rq,Sa,Sq for non-contact profilometer:
The image is leveled with LS-plane to find the primay surface and remove waviness following the ISO 25178
3D image is generated and correlated Sa, Sq values are found
Following the ISO 21920 for roughness profiles, 2 filters are applied (Gaussian S-filter and cut-off wavelength at 2.5 µm and Gaussian L-filter and cut-off wavelength at 0.8 mm from ISO 16610-21)
An option manage end-effects has been applied to visualize the full length despite the computed cut-offs
A particle size analysis has been also carried out through the identification of D10, D50, D90, Span for cumulative distribution and broadness:
The detection method is Watershed for Packed Features with classification only related to particles and smallest boundary width of 4 pixels, related to a 2,5 µm x 2,5 µm section
Shallow features are merged with a 5% range threshold

## Slide 5: Results (top)

## Slide 6: Results (Top)
3UH
4UH
19UH
20UH
5F
6F
21F
22F
9H
10H
12H
13H
11UF
12UF
14UF
15UF

## Slide 9: Particle Size analysis (x10)

## Slide 10: Particle Size analysis (x10)

## Slide 11: Particle Size analysis (x20)

## Slide 12: Particle Size analysis (x10)

## Slide 13: Results (Side)

## Slide 14: Results (Side)

## Slide 15: Particle Size analysis (x20)

## Slide 16: Particle Size analysis (x20)

## Slide 17: Results (Bottom)

## Slide 18: Results (BOttom)

## Slide 19: Particle Size analysis (x20)

## Slide 20: Particle Size analysis (x20)